Table S1. Parameters used for the adsorption-energy DFT calculations.

| Category | Parameter | Value | Unit | Source |
| --- | --- | --- | --- | --- |
| Method | Code / functional | Quantum ESPRESSO; PBE | – | Ref. 48, S1 |
|  | Dispersion / Hubbard U (Ni 3d) | Grimme D3; 6.2 eV | – | Ref. S2, 49 |
|  | Cut-off (wavefunction / charge density) | 60 / 480 | Ry | – |
|  | Smearing (Gaussian) | 0.05 | eV | – |
|  | Convergence (SCF / force) | 1 × 10⁻⁶ Ry / 1 × 10⁻³ Ry bohr⁻¹ | – | – |
|  | k-point mesh (slab / check / molecule) | 2 × 3 × 1 / 3 × 4 × 1 / Γ | – | Γ-centered |
| Surface model | Slab | LiNiO₂(104), 1 × 4, four layers, 192 atoms (Li₄₈Ni₄₈O₉₆) | – | – |
|  | Cell (in-plane × height) | 18.27 × 11.51 × 30.26 | Å | – |
|  | Adsorbate–image separation | > 15 | Å | – |
|  | Constrained atoms | 144 (z ≤ 17.40 Å) | – | – |
|  | Magnetic configuration | Antiferromagnetic (net 0); Ni 1.02 μB | – | – |
|  | Dipole correction | Along surface normal | – | – |
| Adsorbate | SDCP repeat unit (neutral) | C₁₁H₁₆O₆S₂ | – | – |
|  | PTFE segment | C₁₀F₂₂ | – | – |
|  | Gas-phase reference box padding | 20 and 24 | Å | – |
| Configuration search | Potential; sites / orientations; force | UMA-s-1p1; 7 / 48; 0.05 eV Å⁻¹ | – | Ref. S3 |
| Adsorption energy | Definition | Equation (1) | eV | – |

Parameters for the molecular (oligomer) calculations are given in Supplementary Note 2.